## Slide 1: Rate Limiting Step
The heterogeneous catalytic reaction goes through different steps and rates of the three major steps occurring in series (adsorption, surface reaction, desorption) are equal at steady state.
Among these three steps, one step is rate limiting or rate determining step.
If this step goes faster, the overall rate of the process will be faster or rate will be more, and vice-versa.
We consider the heterogeneous process is analogous to an electrical circuit.

## Slide 2: Contd…
EMF E as the driving force which is the concentration difference of the reactant from bulk phase to the catalyst surface
Current I as rate of the reaction (, mol/s. g of catalyst)
Total resistance Rt as the resistance associated with each step in series
Among the three resistances, the value of
one resistance is highest.

## Slide 3: Contd…
The largest resistance in the circuit controls the amount of current passing through it.
Similarly, the step with largest resistance controls rate of the reaction in the heterogeneous catalytic process.
If we can somehow lower the largest resistance of the step, the rate of the reaction will increase.
Hence, the step with largest resistance is the rate limiting step.

## Slide 4: Synthesisng a Rate Law: Rate Limiting Step
The rate limiting step, mechanism of the reaction and the rate law consistent with the experimental observation can be obtained by taking the example of a reaction which is not diffusion controlled.
To find out the rate limiting step, each step (adsorption, surface reaction and desorption) can be assumed as rate limiting one by one and analysed them.
In doing this, Cumene disproportionation reaction is taken as model reaction
Click to add text

## Slide 5: Contd…
Cumene disproportionation reaction catalyed by Pt as solid catalyst
Steps of this heterogeneous reaction:
Each step is considered as elementary step.
Concentration of gas phase is replaced by its partial pressure.

## Slide 6: Rate Law for adsorption limited reaction
Assuming adsorption is rate limiting
To determine this, the rate law following adsorption as rate limiting should be consistent with the experimental data.
Writing the rate expressions of all the steps,
Adsorption: =  =  )
Surface reaction: = = )
Desorption: = = )

## Slide 7: Contd…
At steady state, ===,
In adsorption-limited reaction, << ,
Therefore, >> , ,  0,  0 compared to
Hence, surface reaction can be written as:
= ), = ) = 0,  =
Similarly for desorption,
= ), = ) =0, 

## Slide 8: Contd…
Hence, putting the expression of , we get,
= =
Hence, putting this expression of into the adsorption rate expression,
=  )=  )=  )
Now, when there is no adsorption, we can look at the reaction as,
C  B + P

## Slide 9: Contd…
If and are the forward and reverse rate constants respectively and is the equilibrium constant, then the rate equation can be written as,
= ()
Now, comparing this equation with the adsorption rate equation,
=  ) , we can write,
=
Therefore, the adsorption rate equation can be written as,
=  )

## Slide 10
Now, we have to eliminate using site balance equation,
= + +
= + +
= (1++ )
=
Combining the equations we can write the rate of the reaction as,
= =  ) ()
=  )

## Slide 11
At the initial condition, initial rate () can be determined.
= = ----(1), is the initial pressure of C.
Initially there is no product, hence and are zero.
= constant.
If cumene disproportionation reaction
is adsorption controlled, then the
experimental data should follow
equation (1) and plotting them will
form a straight line passing through origin.

## Slide 12: Surface Reaction Limited Rate Law
As before, we can determine the rate expression for surface reaction when the process is limited by the surface chemical reaction.
= =
writing the initial rate expression where are zero,
Substituting =,
= =
At low partial pressure of cumene, 1>>
 = , so, at this condition, rate linearly varies with partial pressure.

## Slide 13: Contd…
When desorption is the controlling step, plotting experimental data will give a straight line parallel to X axis, which means that the initial rate is independent of the partial pressure of cumene.

## Slide 14: Contd..
At high partial pressure of cumene, 1 <<,
The rate equation is written as = = constant
At this condition, rate is independent of partial pressure.
If the process is surface reaction controlled, then plotting the experimental data will generate the graph as shown here.

## Slide 15: Desorption as Rate Limiting Step
When desorption is assumed as the rate limiting step, the rate equation will be
= =
To determine the dependence of the initial rate on partial pressure of cumene, setting = =0, the rate law reduces to,
= = constant